## Slide 1: Liquid Crystal Elastomer Response to Light
Rafael Soares Zola
CPIP-LCI
Advisor: Peter Palffy-Muhoray

## Slide 2: Objectives
Observe the response of the Liquid Crystal Elastomer (LCE) to a source of light;
Understand the key features of the Spatial Light Modulator (SLM);
Use the SLM as a dynamic element;
Apply light with intensity varying with position and time on the sample;

## Slide 3: Background
Liquid Crystal Elastomer*:
Rubber and Liquid Crystal!
Doped
azo dye Disperse Orange III
Backbone
Mesogen
Cross-Linker (12%)
4.0mm
7.5mm
*M. Camacho-Lopez, et al Nature Materials 3, 307 (2004).

## Slide 4: Background
Change in the degree of order:
  cis-trans transition (Azo Dye)
  temperature
The free energy of the elastomer
rubber
liquid crystal
coupling term

## Slide 5: Background
SLM:
Twisted Nematic cell used as dynamic element in experimental setups

## Slide 6: Background
Computer
Image
Laser through
Transmissive SLM
Number of pixels:832 x 624
Pixel pitch: 32m
Image frame rate: max. 60Hz
Active area: 26.6mm x 20.0mm

## Slide 7: Capability of SLM

## Slide 8: Background
Intensity vs. gray level:

## Slide 9: Setup
Camera
Computer
Analyzer
Lens
Mirror
Sample
Polarizer
Argon Laser
- CW
- =514nm
Filter 514nm

## Slide 10: Setup
Sample
SLM
Camera
Microscope Objective

## Slide 11: Results
Ppump=15mW

## Slide 12: Results
Ppump=15mW
ttransition= 10s

## Slide 13: Results
Ppump=43.73mW
ttransition= 10s

## Slide 14: Conclusions
The SLM can be used to control the intensity over the sample spatially and temporally
This control allows one to move the LCE in some specific manner
Coordinated movements depends on accurate control of the beam over the sample

## Slide 15: Acknowledgements
Especial Thanks for:
Dr. Michele Moreira (muito obrigado mesmo!!)
Jake Fontana
Jeremy Neal