## Slide 1: Measuring Refractive Indices of Nematic LC Elastomers
Volodymyr Borshch
Research advisor: Professor Peter Palffy-Muhoray
25 August 2008

## Slide 2: Outline
Motivation
Nematic LC elastomer
Methods and previous results
Theory
Materials selection
Experimental setup
Obtained data
Conclusions
Acknowledgments

## Slide 3: Motivation
Nematic LC Elastomers have bright future
Not all physical properties are quite extensively described so far
E.g. Refractive index

## Slide 4: Nematic LC elastomer
O
O
O
O
Mesogen
O
CH3
H
CH3
Si
O
CH3
Si
H
CH3
Si
H
85
CH3
Backbone
CH2
O
CH2
O
Crosslinker
From Israel Lazo presentation

## Slide 5: Methods
Israel Lazo presentation
Notes: The results are puzzling
To be confirmed

## Slide 6: Yet another approach
From Fresnel equations:
The main idea of the method R=0

## Slide 7: High refractive index liquids
Liquids at or near 20˚C
Refractive index | Material
1.627 | Quinoline
1.660 | α-Monobromonaphthalene
1.717 | Mercury potassium iodide
1.737 | Methylene iodide
1.78 | Methylene iodide and sulphur (saturated)
1.793 | Barium mercuric iodide aq.
1.82 | Potassium iodide and mercuric iodide aq.
1.868 | Solutions of 35% by weight CH2I2, 31% SnI4, 16% AsI3, 8% SbI3 and 10% S
1.885 | Hydrogen disulphide
1.95 | Phosphorus in carbon disulphide
2.06 | Yellow phosphorus 8 parts by weight + 1part sulphur + 1 methylene iodide
2.2 | Mercuric iodide in aniline or quinoline
Data from Kaye and Laby, Tables of Physical and Chemical Constants, 1959
Ionic liquids based on 1-alkyl-3-methylimidazolium cations
Most of them were either:
- Highly toxic and poisonous - Not transparent - Not available
A simple, cost-effective and magnificent liquid was used – saturated solution of NaI
n = 1.496

## Slide 8: Experiment
HeNe
Rotating polarizer
Fish tank with immersed elastomer
Experimental setup
Measuring the reflectance of the elastomer in normal incidence
λ/4 plate
detector
632.8 nm filter
Reference beam
Beam splitter
lens
Lock-in amplifier
detector

## Slide 9: no measurement
The polarization is perpendicular to the preferred director orientation n
elastomer with no strain
batch #71 (10% cross linkers)
Fitting and extrapolation gives n=1.60365
±0.01633
The sample from batch #69 gave similar value n=1.53529

## Slide 10: ne measurement
The polarization is parallel to the preferred director orientation n
elastomer with no strain
batch #71 (10% cross linkers)
Fitting and extrapolation gives n =1.64128
±0.03830

## Slide 11: Benefits and drawbacks of the method
Looks simple
Inhomogeneity of elastomer
Scattering

## Slide 13: Conclusions
The sample was different but the results agree with previous measurements
The refractive indices need to be measured more accurately
Future work: Generalized Ellipsometry
Need to measure inhomogeneity
Notes: Handbook of Ellipsometry, edited by Harland G. Tompkins, Eugene A. Irene
William Andrew publishing, 2005, ISBN: 0-8155-1499-9
Chapter 9. Theory and Application of Generalized Ellipsometry
by Mathias Schubert

## Slide 14: Acknowledgement
Prof.Peter Palffy-Muhoray
Jake Fontana, Israel Lazo
Paul Luchette, Michele Fontana
Jeremy Neal, Sabrina Relaix
Rafael Zola

## Slide 15: Thank you !