## Slide 1
Liquid Crystal Institute
Israel Lazo, Jeremy Neal and Peter Palffy-Muhoray
Liquid Crystal Institute, Kent State University, Kent OH, 44242
Determination of refractive indices of liquid crystal elastomer

## Slide 2: Motivation and Objectives
Understand the physical properties of this new materials
Measure the individual refractive indices of a nematic liquid crystal elastomer
Determine how this refractive indices change as a function of strain

## Slide 3: LC elastomer
O
O
O
O
Mesogen
O
CH3
H
CH3
Si
O
CH3
Si
H
CH3
Si
H
85
CH3
Backbone
CH2
O
CH2
O
Crosslinker

## Slide 4: Refractive indices
E
k
n
LC
E
k
n
no
ne
Techniques:
Brewster’s angle measurement
Interferometry
LC elastomer

## Slide 5: Brewster’s angle
Schematic diagram of the experimental setup for Brewster’s angle measurements
Holder
-polarization
i
He-Ne
Sample
Detector
n
Brewster’s angle!

## Slide 6: Brewster’s angle (Model)
n
Sample
x
z
E
Vertical configuration
n
Sample
x
z
E
Horizontal configuration
pv

## Slide 7
n

Ei
2
Hi
2
ki
kt
Dt
Et
1
Elastomer’s surface
Er
Mathematical model
s

## Slide 8: Results
Experimental results for Brewster’s angle technique
S increases with strain

## Slide 9: Interferometry
Schematic diagram of the experimental setup for conoscopic interferometer
M: Mirror
L: Lens
L
Sample
M
M
BP
He-Ne
n
E

## Slide 10: Interferometer
Phase shift
Special consideration must be taken when calculating ne
Ordinary refractive index
non2

## Slide 11
Experimental results for Interferometer and Brewster’s angle techniques

## Slide 12: Conclusion
We have measured the ordinary and extraordinary refractive indices of a nematic liquid crystal elastomer using two different methods
Two methods are in a good agreement
To do
Confirm and interpret the results.